## Slide 1: Theory of resonant x-ray spectroscopy; excitons and multiplets
Transition metal and rare earth compounds show a wealth of different properties. May it be as materials for energy storage (battery compounds), dyes in solar cells, elements in the read head of hard-disks, high temperature superconductors, or the active centers in many of the known enzymes. The wealth of properties of these materials is related to the large number of low energy degrees of freedom of the transition metal ion. The local interactions between these often open shell systems lead to these low energy degrees of freedom, but also make these materials involved to understand.
Core level spectroscopy in many cases turns out to be a very efficient method to study the local properties of these systems. With x-ray absorption spectroscopy one can probe the average electronic structure, with resonant x-ray diffraction the ordered electronic structure and with resonant inelastic x-ray scattering the dynamics of low energy excitations. For the understanding of these spectra, in this class of materials, it is important to realize that one needs to treat the interactions between the electrons beyond mean field approximations. It is not sufficient to assume independent electrons interacting with an average potential, but one has to consider the interaction between each pair of electrons explicitly. In the spectra this leads to excitons and multiplets that dominate the spectral line-shape. Within the lecture I will introduce these concepts, in the tutorial I will provide a hands on session calculating core level spectroscopy using a code in Mathematica.

## Slide 2
Theory of resonant x-ray spectroscopy;
excitons and multiplets
http://www.thphys.uni-heidelberg.de/~haverkort/talks/start
Maurits W. Haverkort
Institute for theoretical physics – Heidelberg University
M.W.Haverkort@thphys.uni-heidelberg.de
Positions available

## Slide 3
Challenges in solid state physics / chemistry
Important for technology
Important in biochemistry (active centers of enzymes)
Often open shell systems, involved to understand

## Slide 4
Transition metal compounds; a large variety of properties
Metal insulator transitions
M. Marezio et al.,
PRB 5, 2541 (1972)
P. B. Allen et al.,
PRB 48, 4359 (1993)
VO2
Resistivity (Wcm)

## Slide 5
Transition metal compounds; a large variety of properties
High-Tc superconductivity

## Slide 6
Transition metal compounds; a large variety of properties
Active centers in enzymes
Fe in Heme
Mn role in photosynthesis

## Slide 7
Spin
Orbital
Lattice
Charge
Interaction between the charge, lattice, orbital and spin

## Slide 8
Spin arrangements (element resolved of TM multilayers)
Valence and local symmetry of TM compounds
Orbital occupation (the d-shell is 5 fold degenerate)
dyz
dxz
dxy
dx2-y2
d3z2-r2
Need tools to measure
And excitations (spin-waves – magnons – orbital excitations)
Spectroscopy
(x-ray spectroscopy)
Notes: ----- Meeting Notes (12/7/12 18:14) -----
Outline
link between them
Spin orbital physics
- Dispersion
- Local occupation, ground state wavefunction
- spatial extend

## Slide 9
A) At some point in time the photon gets absorbed, the photon disappears and the electron in the s-shell is excited to the p-shell
Quiz: what happens when a photon hits an atom?
For example an H atom with one electron in the s-shell
B) Photons are electromagnetic waves. The electron starts to oscillate around the nucleus with the photon frequency
C) Photons are particles. The photon bounces like a ball of the electron, thereby transferring part of its energy to the electron
Notes: I know that the 1s to 2p excitation of H is not in the x-ray range ( ¾ Rydberg, 10.2 eV) but all our theories are conveniently rather independent from the actual energy scale. (Linear response does not depend on the value of omega) For the purist replace H by Fe25+ (also a single electron around a nucleus, but as Z=26 in this case the excitation energy is 26^2 * ¾ = 507 Rydberg or 6898 eV)

## Slide 10
Interaction of photons with matter

## Slide 11
Interaction of photons with matter

## Slide 12
Need tools to measure: Orbital, Spin, Charge
2p
X-ray Absorption Spectroscopy (XAS) at the TM 2p to 3d edge
Technique developed in late 1980’s
Fink, Sawatzky, Fuggle
Thole, van der Laan
Chen, Sette

## Slide 13
Resonant X-ray Diffraction (RXD)
2p
Need tools to measure: Orbital, Spin, Charge
X-ray Absorption Spectroscopy (XAS) at the TM 2p to 3d edge
Hannon, Trammel, Bloom, Gibbs
Phys. Rev. Lett. 61, 1245 (1988)
Phys. Rev. B 43, 5663 (1991)
Cara, Thole
Rev. Mod. Phys. 66, 1509 (1994)

## Slide 14
Resonant X-ray Diffraction (RXD)
Resonant Inelastic X-ray Scattering (RIXS)
Need tools to measure: Orbital, Spin, Charge
X-ray Absorption Spectroscopy (XAS) at the TM 2p to 3d edge
Theory prediction of magnetic excitations
J. Luo, G. T. Trammell, and J. P. Hannon,
Phys. Rev. Lett. 71, 287 (1993).
F.M.F. de Groot, P. Kuiper, and G. A. Sawatzky,
Phys. Rev. B 57, 14584 (1998).
Experimental realization
L. Braicovich, G. Ghiringhelli, N. B. Brookes, et al.
Phys. Rev. Lett. 102, 167401 (2009).
2p
Notes: ----- Meeting Notes (12/7/12 17:29) -----
Quantitative (real might be offending ...)
----- Meeting Notes (12/7/12 18:14) -----
What did I do
Development of model based on DFT wannier

## Slide 15
non-resonant Inelastic X-ray Scattering (IXS)
3p
Need tools to measure: Orbital, Spin, Charge
X-ray Absorption Spectroscopy (XAS) at the TM 2p to 3d edge
Resonant X-ray Diffraction (RXD)
Resonant Inelastic X-ray Scattering (RIXS)
Nobelprize Compton
Light elements – band excitations:
Keijo Hämäläinen, W. Schulke
Excitonic excitations TM and RE compounds:
B. C. Larson et al. PRL 99, 026401 (2007)
M. W. Haverkort et al. PRL 99, 257401 (2007)
R. A. Gordon, et al. EPL 81, 26004 (2008)
T. Willers, et al. PRL 109, 046401 (2012)
Notes: wannier

## Slide 16
X-ray Absorption Spectroscopy
2p

## Slide 17
X-ray Absorption Spectroscopy – some observations
Data L. H. Tjeng et al.

## Slide 18
X-ray Absorption Spectroscopy – some observations
2p
Data L. H. Tjeng et al.

## Slide 19
X-ray Absorption Spectroscopy – some observations
Valence dependence – ground state symmetry determines the line shape
Data L. H. Tjeng et al.

## Slide 20
X-ray Absorption Spectroscopy – some observations
2p
Polarized XAS
Sensitive to
Orbital occupation
Natural linear dichroism
C. T. Chen et al PRL 68, 2543 (1992)

## Slide 21
X-ray absorption spectroscopy – Spin sensitive
2p
700
720
740
760
Photon energy (eV)
Polarized XAS
Sensitive to
Magnetic moments
Magnetic circular dichroism
J. Stöhr, J. Elec. Spec. Rel. Phonom. 75, 253 (1995).

## Slide 22
X-ray Absorption Spectroscopy – some observations
Polarized XAS
Sensitive to
Magnetic moments
Magnetic linear dichroism
2p
P. Kuiper et al., PRL 70, 1549 (1993)

## Slide 23
X-ray absorption spectroscopy – a band picture
1s

## Slide 24
X-ray absorption spectroscopy – one electron selection rules
Fermi’s golden rule
The math simplifies with the use of Green’s functions

## Slide 25
X-ray absorption spectroscopy – one electron selection rules
Fermi’s golden rule
The math simplifies with the use of Green’s functions

## Slide 26
X-ray absorption spectroscopy – one electron selection rules
Fermi’s golden rule
The math simplifies with the use of Green’s functions

## Slide 27
X-ray absorption spectroscopy – one electron selection rules

## Slide 28
X-ray absorption spectroscopy – one electron selection rules

## Slide 29
X-ray absorption spectroscopy – one electron selection rules

## Slide 30
X-ray absorption spectroscopy – one electron selection rules
C. T. Chen et al. Phys. Rev. Lett. 68, 2543 (1992)

## Slide 31
X-ray absorption spectroscopy – correlations in the d-shell
Energy (eV)
Intensity
2p

## Slide 32
Use NiO as an example material
Ni2+ - 4s0 3d8
O2- - 2p6

## Slide 33
Partly filled degenerate d-shell – in LDA NiO is a metal

## Slide 34
X-ray absorption spectroscopy – correlations in the d-shell
2p
Experiment is sharper than LDA empty density of states
Branching ratio (L2, L3 intensity ratio is not 3:2)
Experiment shows more structure (multiplets) than DOS

## Slide 35
X-ray absorption spectroscopy – correlations in the d-shell
2p
Experiment is sharper than LDA empty density of states
Branching ratio (L2, L3 intensity ratio is not 3:2)
Experiment shows more structure (multiplets) than DOS

## Slide 36
In LDA NiO is a metal: Experimentally it is a good insulator
F. J. Morin, Phys. Rev. 93, 1199 (1954)
R. Newman and R. M. Chrenko,
Phys. Rev 114 1507 (1959)
Room temperature
r~105 O cm
Optical-gap
3.5 – 4.0 eV
Conductivity (W-1 cm-1)
Temperature-1

## Slide 37
Mott-Hubbard insulator
Energy gain W
Energy cost U
Difference between anti-ferromagnetic Neel order and spin-singlet configurations
vs.

## Slide 38
Mott-Hubbard insulator
Keep all correlations on a single central site – use a (dynamical) mean-field approximation for the rest of the solid.

## Slide 39
X-ray absorption spectroscopy – correlations in the d-shell
Energy (eV)
Intensity
2p
W=1
U=0
Y. Lu, M. Höppner, O. Gunnarsson, M.W. Haverkort, PRB 90, 085102 (2014)

## Slide 40
X-ray absorption spectroscopy – correlations in the d-shell
Energy (eV)
Intensity
2p
W=1
U=0.25
Y. Lu, M. Höppner, O. Gunnarsson, M.W. Haverkort, PRB 90, 085102 (2014)

## Slide 41
X-ray absorption spectroscopy – correlations in the d-shell
Energy (eV)
Intensity
2p
W=1
U=0.5
Y. Lu, M. Höppner, O. Gunnarsson, M.W. Haverkort, PRB 90, 085102 (2014)

## Slide 42
X-ray absorption spectroscopy – correlations in the d-shell
Energy (eV)
Intensity
2p
W=1
U=1.0
Y. Lu, M. Höppner, O. Gunnarsson, M.W. Haverkort, PRB 90, 085102 (2014)

## Slide 43
X-ray absorption spectroscopy – correlations in the d-shell
Energy (eV)
Intensity
2p
W=1
U=1.5
Y. Lu, M. Höppner, O. Gunnarsson, M.W. Haverkort, PRB 90, 085102 (2014)

## Slide 44
X-ray absorption spectroscopy – correlations in the d-shell
Energy (eV)
Intensity
2p
W=1
U=2.0
Y. Lu, M. Höppner, O. Gunnarsson, M.W. Haverkort, PRB 90, 085102 (2014)

## Slide 45
X-ray absorption spectroscopy – correlations in the d-shell
Energy (eV)
Intensity
W=1
U=2.0
2p
Y. Lu, M. Höppner, O. Gunnarsson, M.W. Haverkort, PRB 90, 085102 (2014)

## Slide 46
X-ray absorption spectroscopy – excitons
Energy (eV)
Intensity
2p
Core – valence interaction
W=1
U=20
Q=0
M.W. Haverkort, G. Sangiovanni, P. Hansmann, A. Toschi, Y. Lu, S. Macke EPL, 108 57004 (2014)

## Slide 47
X-ray absorption spectroscopy – excitons
Energy (eV)
Intensity
2p
W=1
U=20
Q=0.25
M.W. Haverkort, G. Sangiovanni, P. Hansmann, A. Toschi, Y. Lu, S. Macke EPL, 108 57004 (2014)

## Slide 48
X-ray absorption spectroscopy – excitons
Energy (eV)
Intensity
2p
W=1
U=20
Q=0.5
M.W. Haverkort, G. Sangiovanni, P. Hansmann, A. Toschi, Y. Lu, S. Macke EPL, 108 57004 (2014)

## Slide 49
X-ray absorption spectroscopy – excitons
Energy (eV)
Intensity
2p
W=1
U=20
Q=1.0
M.W. Haverkort, G. Sangiovanni, P. Hansmann, A. Toschi, Y. Lu, S. Macke EPL, 108 57004 (2014)

## Slide 50
X-ray absorption spectroscopy – excitons
Energy (eV)
Intensity
2p
W=1
U=20
Q=1.25
M.W. Haverkort, G. Sangiovanni, P. Hansmann, A. Toschi, Y. Lu, S. Macke EPL, 108 57004 (2014)
Notes: ----- Meeting Notes (12/7/12 17:29) -----
Quantitative (real might be offending ...)
----- Meeting Notes (12/7/12 18:14) -----
What did I do
Development of model based on DFT wannier

## Slide 51
X-ray absorption spectroscopy – excitons
Energy (eV)
Intensity
2p
W=1
U=20
Q=1.5
M.W. Haverkort, G. Sangiovanni, P. Hansmann, A. Toschi, Y. Lu, S. Macke EPL, 108 57004 (2014)
Notes: ----- Meeting Notes (12/7/12 17:29) -----
Quantitative (real might be offending ...)
----- Meeting Notes (12/7/12 18:14) -----
What did I do
Development of model based on DFT wannier

## Slide 52
X-ray absorption spectroscopy – excitons
Energy (eV)
Intensity
2p
W=1
U=20
Q=1.75
M.W. Haverkort, G. Sangiovanni, P. Hansmann, A. Toschi, Y. Lu, S. Macke EPL, 108 57004 (2014)

## Slide 53
X-ray absorption spectroscopy – excitons
Energy (eV)
Intensity
2p
W=1
U=20
Q=2.0
Exciton
Continuum edge jump
M.W. Haverkort, G. Sangiovanni, P. Hansmann, A. Toschi, Y. Lu, S. Macke EPL, 108 57004 (2014)

## Slide 54
X-ray absorption spectroscopy – excitons
2p

## Slide 55
X-ray absorption spectroscopy – excitons
2p

## Slide 56
Local many body calculations based on parameters

## Slide 57
Ligand field theory for NiO
Ni2+ - 4s0 3d8
O2- - 2p6

## Slide 58
Orbital energy level diagram
t2g
eg

## Slide 59
Coulomb repulsion
dxy
dx2-y2
Notes: ----- Meeting Notes (12/7/12 17:29) -----
Quantitative (real might be offending ...)
----- Meeting Notes (12/7/12 18:14) -----
What did I do
Development of model based on DFT wannier

## Slide 60
Coulomb repulsion
dxy
dx2-y2
dz2
Coulomb repulsion is smaller when electrons are farther apart

## Slide 61
Coulomb repulsion
dx2-y2
dz2
dxy
dxy
Coulomb repulsion is smaller when electrons are farther apart
Notes: ----- Meeting Notes (12/7/12 17:29) -----
Quantitative (real might be offending ...)
----- Meeting Notes (12/7/12 18:14) -----
What did I do
Development of model based on DFT wannier

## Slide 62
XAS final state for NiO 2p53d9
Ni – 2p
Ni – 3d
L3 edge
L2 edge

## Slide 63
Local many body calculations based on parameters
Parameters
Size of the Coulomb interaction
Size of the crystal-field

## Slide 64
Can we calculate these parameters?
Parameters
Size of the Coulomb interaction
Size of the crystal-field
Notes: -

## Slide 65
Obtain parameters from LDA
M.W. Haverkort, M. Zwierzycki, O.K. Andersen, PRB 85, 165113 (2012).

## Slide 66
In LDA NiO is a metal: Experimentally it is a good insulator
F. J. Morin, Phys. Rev. 93, 1199 (1954)
R. Newman and R. M. Chrenko,
Phys. Rev 114 1507 (1959)
Room temperature
r~105 O cm
Optical-gap
3.5 – 4.0 eV
Conductivity (W-1 cm-1)
Temperature-1

## Slide 67
Although NiO is a metal in LDA, there are many things correct
M.W. Haverkort, M. Zwierzycki, O.K. Andersen, PRB 85, 165113 (2012).

## Slide 68
“Downfold” the DFT results to obtain basis of choice
M.W. Haverkort, M. Zwierzycki, O.K. Andersen, PRB 85, 165113 (2012).

## Slide 69
Pick a basis of “TM-d” and “O-p” Wannier orbitals
M.W. Haverkort, M. Zwierzycki, O.K. Andersen, PRB 85, 165113 (2012).

## Slide 70
Full multiplet ligand field model based on DFT
M.W. Haverkort, M. Zwierzycki, O.K. Andersen, PRB 85, 165113 (2012).

## Slide 71
How to calculate 2p X-ray Absorption Spectroscopy
2p
Start from LDA potential
Create Wannier functions
On this basis and potential build local Hamiltonian including all local many body interactions
Solve by exact diagonalization
Phys. Rev. B 85, 165113 (2012)
Theory
Experiment
M.W. Haverkort, M. Zwierzycki, O.K. Andersen, PRB 85, 165113 (2012).

## Slide 72
Interpretation without theory – sum rules
2p
Theory
Experiment

## Slide 73
Sum rules for circular dichroism: orbital and spin momentum

## Slide 74
Sum rules for circular dichroism: orbital and spin momentum

## Slide 75
Sum rules for circular dichroism: orbital and spin momentum

## Slide 76
Sum rules for circular dichroism: orbital and spin momentum

## Slide 77
Sum rules for circular dichroism: orbital and spin momentum

## Slide 78
Sum rules for circular dichroism: orbital and spin momentum

## Slide 79
Sum rules for linear dichroism: orbital occupation

## Slide 80
XAS and the conductivity tensor (s) – an example for s to p
w0
Real
Imaginary
Absorption –Im[s]
(in Landau Lifschitz absorption is Re[s])

## Slide 81
But the conductivity tensor (s) is a TENSOR

## Slide 82
But the conductivity tensor (s) is a TENSOR
Absorption
–Im[e.s.e]

## Slide 83
The conductivity tensor (s) in cubic symmetry

## Slide 84
The conductivity tensor (s) in tetragonal symmetry

## Slide 85
The conductivity tensor (s) in orthorhombic symmetry

## Slide 86
The conductivity tensor (s) in monoclinic symmetry

## Slide 87
The conductivity tensor (s) in triclinic symmetry

## Slide 88
The conductivity tensor (s) in magnetic materials

## Slide 89
The conductivity tensor (s) in magnetic materials

## Slide 90
Sum rules for circular dichroism: orbital and spin momentum

## Slide 91
Thole et al.’s sum-rules in tensor form. s to p excitations

## Slide 92
Resonant X-ray Diffraction (RXD)
2p
And now momentum, i.e. spatial resolved, from XAS to RXD
X-ray Absorption Spectroscopy (XAS) at the TM 2p to 3d edge
Hannon, Trammel, Bloom, Gibbs
Phys. Rev. Lett. 61, 1245 (1988)
Phys. Rev. B 43, 5663 (1991)
Cara, Thole
Rev. Mod. Phys. 66, 1509 (1994)

## Slide 93
An example magnetic Bragg reflection of Ho metal film
2p

## Slide 94
An example magnetic Bragg reflection of Ho metal film

## Slide 95
2p
Relation between resonant x-ray diffraction and absorption
2p

## Slide 96
An example magnetic Bragg reflection of Ho metal film

## Slide 97
Fundamental spectra from the literature

## Slide 98
Fundamental spectra from the literature

## Slide 99
Fundamental spectra from the literature

## Slide 100
Fundamental spectra from the literature

## Slide 101
An example magnetic Bragg reflection of Ho metal film

## Slide 102
Can we use sum-rules to get quantitative information
E. Benckiser et al., Nature Materials 10, 189 (2011). S. Macke et al., Advanced Materials 26, 6554 (2014).

## Slide 103
Can we use sum-rules to get quantitative information
E. Benckiser et al., Nature Materials 10, 189 (2011). S. Macke et al., Advanced Materials 26, 6554 (2014).

## Slide 104
Can we use sum-rules to get quantitative information
E. Benckiser et al., Nature Materials 10, 189 (2011). S. Macke et al., Advanced Materials 26, 6554 (2014).

## Slide 105
Can we use sum-rules to get quantitative information
E. Benckiser et al., Nature Materials 10, 189 (2011). S. Macke et al., Advanced Materials 26, 6554 (2014).

## Slide 106
Can we use sum-rules to get quantitative information
E. Benckiser et al., Nature Materials 10, 189 (2011). S. Macke et al., Advanced Materials 26, 6554 (2014).

## Slide 107
Can we use sum-rules to get quantitative information
E. Benckiser et al., Nature Materials 10, 189 (2011). S. Macke et al., Advanced Materials 26, 6554 (2014).

## Slide 108
Solve Maxwell's equations (with side conditions)
E. Benckiser et al., Nature Materials 10, 189 (2011). S. Macke et al., Advanced Materials 26, 6554 (2014).

## Slide 109
2p
2p
And now excitations , from RXD to RIXS
2p
X-ray Absorption
Spectroscopy
Resonant X-ray
Diffraction
Resonant Inelastic
X-ray scattering

## Slide 110
Dispersing magnons

## Slide 111
Dispersing magnons – Neutron scattering
Interaction of Neutrons with matter is well understood (magnetic dipole),
single magnon intensity
q-dispersion
M. T. Hutchings and E. J. Samuelsen,
Phys. Rev. B 6, 3447 (1972)

## Slide 112
Recent development – measure spin dynamics with x-rays
Picture by G. Ghiringhelli and L. Braicovich
Resonant Inelastic
X-ray Scattering
RIXS
It now becomes feasible to measure the dynamics of low energy excitations in:
thin films
surfaces
Interfaces
nano-crystals
molecules

## Slide 113
RIXS – very high quality data on small samples
spinons
orbitons
J. Schlappa et al., Nature 485, 82

## Slide 114
What is Resonant Inelastic X-ray Scattering (RIXS)
Outgoing light of
~ 0.5 to 10 keV
minus
10 meV to 10 eV
Incoming light of
~ 0.5 to 10 keV
Intermediate state with core hole and one extra valence electron
M.W. Haverkort PRL 105, 167404 (2010)

## Slide 115
Intermediate state
RIXS – what does one measure
Initial state
Final state
M.W. Haverkort PRL 105, 167404 (2010)

## Slide 116
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure
M.W. Haverkort PRL 105, 167404 (2010)

## Slide 117
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure
M.W. Haverkort PRL 105, 167404 (2010)

## Slide 118
RIXS – what is the cross section
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
M.W. Haverkort PRL 105, 167404 (2010)

## Slide 119
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure
M.W. Haverkort PRL 105, 167404 (2010)

## Slide 120
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure
M.W. Haverkort PRL 105, 167404 (2010)

## Slide 121
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure
M.W. Haverkort PRL 105, 167404 (2010)

## Slide 122
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure
M.W. Haverkort PRL 105, 167404 (2010)

## Slide 123
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure
M.W. Haverkort PRL 105, 167404 (2010)

## Slide 124
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure
M.W. Haverkort PRL 105, 167404 (2010)

## Slide 125
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
BOOM
RIXS – what does one measure
M.W. Haverkort PRL 105, 167404 (2010)

## Slide 126
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure
M.W. Haverkort PRL 105, 167404 (2010)

## Slide 127
Intermediate state
Initial state
Final state
RIXS – what does one measure

## Slide 128
Relations between absorption, elastic- and inelastic scattering
The elastic scattering tensor is related to the absorption by the optical theorem (Conservation of energy)
Elastic scattering is a limiting case of inelastic scattering:
If one restricts the inelastic scattering operator R to the ground-state one describes the elastic scattering
For the description of magnetic excitations:
Expand the scattering operator on spin operators
M.W. Haverkort PRL 105, 167404 (2010)

## Slide 129
RIXS – effective operator – spin excitations
Effective operator for spin excitations only
M.W. Haverkort PRL 105, 167404 (2010)

## Slide 130
RIXS – effective operator – spin excitations
Need to calculate x-ray absorption spectra
… and spin susceptibilities
M.W. Haverkort PRL 105, 167404 (2010)

## Slide 131
RIXS – effective operator – spin excitations
Need to calculate x-ray absorption spectra
Theory
Experiment
s(0)=
M.W. Haverkort PRL 105, 167404 (2010)

## Slide 132
Predicted RIXS spectra with cross polarized light
spin susceptibility, same as neutron scattering
M.W. Haverkort PRL 105, 167404 (2010)

## Slide 133
General polarization: RIXS is a mixture of 1 and 2 spin flips
M.W. Haverkort PRL 105, 167404 (2010)

## Slide 134
Spin excitations in 1-dimension
S. Glawion et al. PRL 107, 107402 (2011).

## Slide 135
Spin excitations in 1 dimension – Sr2CuO3
J. Schlappa et al., Nature 485, 82

## Slide 136
Dispersing orbitals
spinons
orbitons
J. Schlappa et al., Nature 485, 82

## Slide 137
Dispersing orbitals
J. Schlappa et al., Nature 485, 82

## Slide 138
Dispersing orbitals
J. Schlappa et al., Nature 485, 82

## Slide 139
Additional literature
Core level spectroscopy of Solids
Frank M. F. de Groot and Akio Kotani
NEXAFS Spectroscopy
Joachim Stöhr
Introduction to ligand field theory (chapter 1 – 6)
Carl Johan Ballhausen (1962)
Physical Chemistry (chapter 13 – 18, (10 – 15) edition 5 (8))
Peter Atkins (2006)

## Slide 140
Software to do multiplet calculations
Quanty
www.quanty.org
Quanty is a script language which allows the user to program quantum mechanical problems in second quantization and when possible solve these. It can be used in quantum chemistry as post Hartree-Fock or in one of the LDA++ schemes. (self consistent field, configuration interaction, coupled cluster, restricted active space, ...) The idea of Quanty is that the user can focus on the model and its physical or chemical meaning. Quanty will take care of the mathematics.

## Slide 141
Notes: CONCLUSIONS

## Slide 142
Notes: CONCLUSIONS

## Slide 143
Ligand field theory for NiO
Ni2+ - 4s0 3d8
O2- - 2p6

## Slide 144
Orbital energy level diagram
t2g
eg

## Slide 145
Coulomb repulsion
dxy
dx2-y2
Notes: ----- Meeting Notes (12/7/12 17:29) -----
Quantitative (real might be offending ...)
----- Meeting Notes (12/7/12 18:14) -----
What did I do
Development of model based on DFT wannier

## Slide 146
Coulomb repulsion
dxy
dx2-y2
dz2
Coulomb repulsion is smaller when electrons are farther apart

## Slide 147
Coulomb repulsion
dx2-y2
dz2
dxy
dxy
Coulomb repulsion is smaller when electrons are farther apart
Notes: ----- Meeting Notes (12/7/12 17:29) -----
Quantitative (real might be offending ...)
----- Meeting Notes (12/7/12 18:14) -----
What did I do
Development of model based on DFT wannier

## Slide 148
Coulomb repulsion

## Slide 149
Coulomb repulsion

## Slide 150
Coulomb repulsion
Notes: ----- Meeting Notes (12/7/12 17:29) -----
Quantitative (real might be offending ...)
----- Meeting Notes (12/7/12 18:14) -----
What did I do
Development of model based on DFT wannier

## Slide 151
Coulomb repulsion

## Slide 152
Slater integrals – a multipole expansion

## Slide 153
Slater integrals – a multipole expansion

## Slide 154
Screening of mulitpole Coulomb interaction is small

## Slide 155
-2 | -1 | 0 | 1 | 2
Lz=-2 Sz=1
L=? S=1
3?
Coulomb repulsion in spherical symmetry – Atomic multiplets
Orbital occupation
-2 | -1 | 0 | 1 | 2
d1 (d9)
ml
Lz=-2 Sz=1/2
L=2 S=1/2
Angular momentum
Term symbol
(2S+1)L
2D
-2 | -1 | 0 | 1 | 2
d2 (d8)
ml
Lz=-3 Sz=1
L=3 S=1
3F

## Slide 156
-2 | -1 | 0 | 1 | 2
Lz=-1 Sz=0
Coulomb repulsion in spherical symmetry – Atomic multiplets
Orbital occupation
Angular momentum
-2 | -1 | 0 | 1 | 2
Lz=-2 Sz=1
-2 | -1 | 0 | 1 | 2
d2 (d8)
ml
Lz=-3 Sz=1
There are 5*4/2=10 ways to place two spin up electrons in 5 orbitals
10 Triplets
There are 5*5=25 ways to place a spin up and a spin down electron in 5 orbitals
25 – 10 = 15 singlets

## Slide 157
Coulomb repulsion in spherical symmetry – Atomic multiplets
Orbital occupation
Lz=-3 to 3
Sz=-1 to 1
Angular momentum
Term symbol
(2S+1)L
3F
There are
(2L+1)(2S+1) = 7*3 = 21
states in the 3F term

## Slide 158
-2 | -1 | 0 | 1 | 2
Lz=-1 Sz=1
3P
-2 | -1 | 0 | 1 | 2
Lz=-1 Sz=1
3F
-2 | -1 | 0 | 1 | 2
Lz=-2 Sz=1
L=3 S=1
3F
-2 | -1 | 0 | 1 | 2
d2 (d8)
ml
Lz=-3 Sz=1
L=3 S=1
3F
Coulomb repulsion in spherical symmetry – Atomic multiplets
Orbital occupation
Angular momentum
Term symbol
(2S+1)L
}

## Slide 159
Coulomb repulsion in spherical symmetry – Atomic multiplets
Lz=-3 to 3
Sz=-1 to 1
Angular momentum
Term symbol
(2S+1)L
3F
There are
(2L+1)(2S+1) = 7*3 = 21
states in the 3F term
Lz=-1 to 1
Sz=-1 to 1
3P
There are
(2L+1)(2S+1) = 3*3 = 9
states in the 3P term
3F 3P 1G 1D 1S

## Slide 160
Energy level diagram
3F – F0 – 8/49 F2 – 1/49 F4
1D – F0 – 3/49 F2 + 4/49 F4
3P – F0 + 7/49 F2 – 4/21 F4
1G – F0 + 4/49 F2 + 1/441 F4
1S – F0 + 14/49 F2 + 2/7 F4

## Slide 161
Energy level diagram
t2g
eg

## Slide 162
Lowest state 3A2

## Slide 163
First excited state at ~ 1.1 eV 3T2

## Slide 164
Second excited state at ~1.8 eV 3T2

## Slide 165
Third excited state at ~2.0 eV 1E

## Slide 166
…

## Slide 167
Last d – d excited state 1A1

## Slide 168
Compare to experiment

## Slide 169
Bare Coulomb interactions
Use either F0 from experiment or constraint RPA

## Slide 170
Resulting multiplet splitting in spherical symmetry

## Slide 171
Multiplet splitting v.s. band width

## Slide 172
Multiplet splitting v.s. one particle energy level diagram