## Slide 1: Core level spectroscopy of transition metal and rare earth compounds
Transition metal and rare earth compounds show a wealth of different properties. They are used as materials for energy storage (battery compounds), dyes in solar cells, elements in the read head of hard disks, high temperature superconductors, or the active centers in many of the known enzymes. The large variety of tunable properties of these materials is related to the large number of low energy degrees of freedom of the transition metal or rare earth ion. Correlations between the electrons in a solid lead to a detailed interplay between the local spin, charge, orbital and lattice degrees of freedom. The result is extremely rich physics of these open shell systems. At the same time the interplay between several low energy degrees of freedom make these materials involved to understand. Although enormous theoretical progress has been made during the last years in the understanding of correlated materials one often needs experimental input to understand particular phenomenon.
Core level spectroscopy in many cases turns out to be a very efficient method to study the many body properties of these systems. Core level photoelectron spectroscopy allows one to determine how the low energy Hamiltonian arises from the high-energy scale interactions. It thus provides information on the low energy model parameters of the system. X-ray absorption spectroscopy contains information on the local electronic structure. It provides information on the symmetry of the wave function, such as the local spin-state or orbital occupation. Resonant x-ray diffraction is related to x-ray absorption, in addition to x-ray absorption it allows one to study the special dependence of local electronic order in the system. Resonant inelastic x-ray scattering allows one to study the dynamics of low energy excitations. Non-resonant inelastic x-ray scattering of core level excitations is a technique rather comparable to x-ray absorption spectroscopy with the difference that it allows for non-dipole transitions, useful in the study of involved orbital or multipole ordering.
For the understanding of these spectra, in this class of materials, it is important to realize that one needs to treat the interactions between the electrons beyond mean field approximations. It is not sufficient to assume independent electrons interacting with an average potential, but one has to consider the interaction between each pair of electrons explicitly. In the spectra, this leads to excitons and multiplets that dominate the spectral line-shape.
In this talk I will discuss these various forms of core level spectroscopy, which material properties one can obtain with these techniques and how to theoretically understand these spectra. During the tutorial, I will introduce Quanty, (www.quanty.org) a versatile many body quantum script language that allows one to relatively easily write small programs that can calculate core level spectra of a variety of materials using different levels of approximation or models.

## Slide 2
Core level spectroscopy
of transition metal and rare earth compounds
http://www.thphys.uni-heidelberg.de/~haverkort/teaching/
Maurits W. Haverkort
Institute for theoretical physics, Heidelberg University, Heidelberg, Germany
M.W.Haverkort@thphys.uni-heidelberg.de

## Slide 3
A) At some point in time the photon gets absorbed, the photon disappears and the electron in the s-shell is excited to the p-shell
Quiz: what happens when a photon hits an atom?
For example an H atom with one electron in the s-shell
B) Photons are electromagnetic waves. The electron starts to oscillate around the nucleus with the photon frequency
C) Electrons are particles. The photon bounces like a ball of the electron, thereby transferring part of its energy to the electron
Notes: I know that the 1s to 2p excitation of H is not in the x-ray range ( ¾ Rydberg, 10.2 eV) but all our theories are conveniently rather independent from the actual energy scale. (Linear response does not depend on the value of omega) For the purist replace H by Fe25+ (also a single electron around a nucleus, but as Z=26 in this case the excitation energy is 26^2 * ¾ = 507 Rydberg or 6898 eV)

## Slide 4
Interaction of photons with matter
RIXS
nIXS

## Slide 5
Interaction of photons with matter
RIXS
nIXS

## Slide 6
Final state
Initial state
Energy conservation
Response theory (linear)
Fermi’s golden rule

## Slide 7
Response theory (linear)
Fermi’s golden rule
The math simplifies with the use of Green’s functions

## Slide 8
Response theory (linear)
Fermi’s golden rule
The math simplifies with the use of Green’s functions

## Slide 9
Response theory (linear)
Fermi’s golden rule
The math simplifies with the use of Green’s functions

## Slide 10
First order response functions
Response theory
Higher order response functions (two photon, second order)

## Slide 11
Second talk
RXD
RIXS
nIXS
XAS

## Slide 12
Need tools to measure: Orbital, Spin, Charge
2p
X-ray Absorption Spectroscopy (XAS) at the TM 2p to 3d edge
Technique developed in late 1980’s
Fink, Sawatzky, Fuggle
Thole, van der Laan
Chen, Sette

## Slide 13
Resonant X-ray Diffraction (RXD)
2p
Need tools to measure: Orbital, Spin, Charge
X-ray Absorption Spectroscopy (XAS) at the TM 2p to 3d edge
Hannon, Trammel, Bloom, Gibbs
Phys. Rev. Lett. 61, 1245 (1988)
Phys. Rev. B 43, 5663 (1991)
Cara, Thole
Rev. Mod. Phys. 66, 1509 (1994)

## Slide 14
Resonant X-ray Diffraction (RXD)
Resonant Inelastic X-ray Scattering (RIXS)
Need tools to measure: Orbital, Spin, Charge
X-ray Absorption Spectroscopy (XAS) at the TM 2p to 3d edge
Theory prediction of magnetic excitations
J. Luo, G. T. Trammell, and J. P. Hannon,
Phys. Rev. Lett. 71, 287 (1993).
F.M.F. de Groot, P. Kuiper, and G. A. Sawatzky,
Phys. Rev. B 57, 14584 (1998).
Experimental realization
L. Braicovich, G. Ghiringhelli, N. B. Brookes, et al.
Phys. Rev. Lett. 102, 167401 (2009).
2p

## Slide 15
non-resonant Inelastic X-ray Scattering (IXS)
3p
Need tools to measure: Orbital, Spin, Charge
X-ray Absorption Spectroscopy (XAS) at the TM 2p to 3d edge
Resonant X-ray Diffraction (RXD)
Resonant Inelastic X-ray Scattering (RIXS)
Nobelprize Compton
Light elements – band excitations:
Keijo Hämäläinen, W. Schulke
Excitonic excitations TM and RE compounds:
B. C. Larson et al. PRL 99, 026401 (2007)
M. W. Haverkort et al. PRL 99, 257401 (2007)
R. A. Gordon, et al. EPL 81, 26004 (2008)
T. Willers, et al. PRL 109, 046401 (2012)

## Slide 16
3p
non-resonant Inelastic X-ray Scattering (IXS)
X-ray Absorption Spectroscopy (XAS) at the TM 2p to 3d edge

## Slide 17
Back to XAS
X-ray Absorption Spectroscopy (XAS) at the TM 2p to 3d edge
2p
Technique developed in late 1980’s
Fink, Sawatzky, Fuggle
Thole, van der Laan
Chen, Sette

## Slide 18
Two ways to calculate XAS

## Slide 19
Two ways to calculate XAS – bands
1s

## Slide 20
Two ways to calculate XAS – excitons
2p
Start from LDA potential
Create Wannier functions
On this basis and potential build local Hamiltonian including all local many body interactions
Solve by exact diagonalization
Phys. Rev. B 85, 165113 (2012)
Theory
Experiment

## Slide 21
Interpretation without theory – sum rules
2p
Theory
Experiment

## Slide 22
Sum rules for circular dichroism: orbital and spin momentum

## Slide 23
Sum rules for circular dichroism: orbital and spin momentum

## Slide 24
Sum rules for circular dichroism: orbital and spin momentum

## Slide 25
Sum rules for circular dichroism: orbital and spin momentum

## Slide 26
Sum rules for circular dichroism: orbital and spin momentum

## Slide 27
Sum rules for circular dichroism: orbital and spin momentum

## Slide 28
Sum rules for linear dichroism: orbital occupation

## Slide 29
XAS and the conductivity tensor (s) – an example for s to p
w0
Real
Imaginary
Absorption –Im[s]
(in Landau Lifschitz absorption is Re[s])

## Slide 30
But the conductivity tensor (s) is a TENSOR

## Slide 31
But the conductivity tensor (s) is a TENSOR
Absorption
–Im[e.s.e]

## Slide 32
But the conductivity tensor (s) is a TENSOR
Spectrum measured with
x-polarized light

## Slide 33
But the conductivity tensor (s) is a TENSOR
Spectrum measured with
y-polarized light

## Slide 34
But the conductivity tensor (s) is a TENSOR
Spectrum measured with
z-polarized light

## Slide 35
But the conductivity tensor (s) is a TENSOR
Spectrum measured with
(y+z)-polarized light

## Slide 36
But the conductivity tensor (s) is a TENSOR
Spectrum measured with
(y+z)-polarized light
½

## Slide 37
But the conductivity tensor (s) is a TENSOR
Spectrum measured with
(y+z)-polarized light
½

## Slide 38
But the conductivity tensor (s) is a TENSOR
Spectrum measured with
(y+z)-polarized light
½

## Slide 39
But the conductivity tensor (s) is a TENSOR
Spectrum measured with
(y+z)-polarized light
½

## Slide 40
The conductivity tensor (s) in cubic symmetry

## Slide 41
The conductivity tensor (s) in tetragonal symmetry

## Slide 42
The conductivity tensor (s) in orthorhombic symmetry

## Slide 43
The conductivity tensor (s) in monoclinic symmetry

## Slide 44
The conductivity tensor (s) in triclinic symmetry

## Slide 45
The conductivity tensor (s) in magnetic materials

## Slide 46
The conductivity tensor (s) in magnetic materials

## Slide 47
Sum rules for circular dichroism: orbital and spin momentum

## Slide 48
Thole et al.’s sum-rules in tensor form. s to p excitations

## Slide 49
Resonant X-ray Diffraction (RXD)
2p
And now momentum, i.e. spatial resolved, from XAS to RXD
X-ray Absorption Spectroscopy (XAS) at the TM 2p to 3d edge
Hannon, Trammel, Bloom, Gibbs
Phys. Rev. Lett. 61, 1245 (1988)
Phys. Rev. B 43, 5663 (1991)
Cara, Thole
Rev. Mod. Phys. 66, 1509 (1994)

## Slide 50
An example magnetic Bragg reflection of Ho metal film
2p

## Slide 51
An example magnetic Bragg reflection of Ho metal film

## Slide 52
Absorption and diffraction – two sides of the same coin

## Slide 53
Crystalline sollid
Absorption and diffraction – two sides of the same coin
si
si
si
si
Each site gets polarized by the photon field and the local charge density starts to oscillate.
Absorption
Scattering

## Slide 54
2p
Relation between resonant x-ray diffraction and absorption
2p

## Slide 55
Diffraction at given momentum determined by the sum of local scattering with correct phase:
Crystalline sollid
Absorption and diffraction – two sides of the same coin
si
si
si
si
Each site gets polarized by the photon field and the local charge density starts to oscillate.
Absorption
Scattering

## Slide 56
An example magnetic Bragg reflection of Ho metal film

## Slide 57
Fundamental spectra from the literature

## Slide 58
Fundamental spectra from the literature

## Slide 59
Fundamental spectra from the literature

## Slide 60
Fundamental spectra from the literature

## Slide 61
An example magnetic Bragg reflection of Ho metal film

## Slide 62
Can we use sum-rules to get quantitative information

## Slide 63
Can we use sum-rules to get quantitative information

## Slide 64
Can we use sum-rules to get quantitative information

## Slide 65
Can we use sum-rules to get quantitative information

## Slide 66
Can we use sum-rules to get quantitative information

## Slide 67
Can we use sum-rules to get quantitative information

## Slide 68
Solve Maxwell's equations (with side conditions)

## Slide 69
2p
2p
And now excitations , from RXD to RIXS
2p
X-ray Absorption
Spectroscopy
Resonant X-ray
Diffraction
Resonant Inelastic
X-ray scattering

## Slide 70
Dispersing magnons

## Slide 71
Dispersing magnons – Neutron scattering
Interaction of Neutrons with matter is well understood (magnetic dipole),
single magnon intensity
q-dispersion
M. T. Hutchings and E. J. Samuelsen,
Phys. Rev. B 6, 3447 (1972)

## Slide 72
Recent development – measure spin dynamics with x-rays
Picture by G. Ghiringhelli and L. Braicovich
Resonant Inelastic
X-ray Scattering
RIXS
It now becomes feasible to measure the dynamics of low energy excitations in:
thin films
surfaces
Interfaces
nano-crystals
molecules

## Slide 73
RIXS – very high quality data on small samples
spinons
orbitons

## Slide 74
What is Resonant Inelastic X-ray Scattering (RIXS)
Outgoing light of
~ 0.5 to 10 keV
minus
10 meV to 10 eV
Incoming light of
~ 0.5 to 10 keV
Intermediate state with core hole and one extra valence electron

## Slide 75
Intermediate state
RIXS – what does one measure
Initial state
Final state

## Slide 76
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 77
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 78
RIXS – what is the cross section
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…

## Slide 79
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 80
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 81
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 82
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 83
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 84
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 85
XAS – XRD – RIXS – a time dependent picture

## Slide 86
XAS – XRD – RIXS – a time dependent picture in NiO
eg
t2g

## Slide 87
NiO – Ni 2p to Ni 3d excitation
eg
t2g
Ni-3d and O-2p on level of DMFT. (locally all interactions included)
Ni-3d and Ni-2p Coulomb interactions are local and included
After excitation Auger decay is possible, and included:
Ni-3d, Ni-3p, or Ni-3s scatters into the Ni-2p core hole and a Ni-3d, Ni-3p or Ni-3s orbital is emitted into es,p,d,f,g or h orbital

## Slide 88
NiO – Ni 2p to Ni 3d excitation
X-ray absorption of NiO (L23 edge) is well described.
How does the wave-function (charge density) evolve as a function of time when the sample is hit by an x-ray pulse?

## Slide 89
NiO – Ni 2p to Ni 3d excitation
eg
t2g
We include a light field of 1 kV per Angstrom (possible at SLAC) at an energy of 852 eV.
Pulse duration is 100 atto seconds
Upto c7 (4-th-order) response functions are included

## Slide 90
NiO 2p to 3d excitation in the time domain
1 kV Å-1
350 attosecond
holes in Ni 3d-shell
holes in Ni 2p-shell
FWHM 100 as
41 eV
Energy of pulse 852 eV

## Slide 91
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 92
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
BOOM
RIXS – what does one measure

## Slide 93
Interaction of Neutrons with matter is easy (magnetic dipole),
but for resonant inelastic x-ray scattering nothing is obvious.
A lot is known though…
RIXS – what does one measure

## Slide 94
Intermediate state
Initial state
Final state
RIXS – what does one measure

## Slide 95
Relations between absorption, elastic- and inelastic scattering
The elastic scattering tensor is related to the absorption by the optical theorem (Conservation of energy)
Elastic scattering is a limiting case of inelastic scattering:
If one restricts the inelastic scattering operator R to the ground-state one describes the elastic scattering
For the description of magnetic excitations:
Expand the scattering operator on spin operators

## Slide 96
RIXS – effective operator – spin excitations
Effective operator for spin excitations only

## Slide 97
RIXS – effective operator – spin excitations
Need to calculate x-ray absorption spectra
… and spin susceptibilities

## Slide 98
RIXS – effective operator – spin excitations
Need to calculate x-ray absorption spectra
Theory
Experiment
s(0)=

## Slide 99
Predicted RIXS spectra with cross polarized light
spin susceptibility, same as neutron scattering

## Slide 100
General polarization: RIXS is a mixture of 1 and 2 spin flips

## Slide 101
Spin excitations in 1-dimension

## Slide 102
Spin excitations in 1 dimension – Sr2CuO3

## Slide 103
Dispersing orbitals
spinons
orbitons

## Slide 104
Dispersing orbitals

## Slide 105
Dispersing orbitals

## Slide 106
Additional literature
Core level spectroscopy of Solids
Frank M. F. de Groot and Akio Kotani
NEXAFS Spectroscopy
Joachim Stöhr
Introduction to ligand field theory (chapter 1 – 6)
Carl Johan Ballhausen (1962)
Physical Chemistry (chapter 13 – 18, (10 – 15) edition 5 (8))
Peter Atkins (2006)